## Slide 1: The use of polymeric coatings in storage and handling (before processing) as well as pretreatment:
Problematic areas where non-metallics may be a solution
Current coatings used in biofuels Railcars, Storage tanks and Process vessels

## Slide 2: Presenters
Bob.Bernard@akzonobel.com, CSI, CDT
Engineering Solutions Representative
NACE, Level 2 Coating Inspector
Surojit.B.Mukherjee@akzonobel.com
Technical Specialist Manager
NACE, Level 2 Coating Inspector

## Slide 3: Key Facts
Protecting carbon steel tanks from biofuels-based feedstocks is not new – Marine cargo tanks.
Track Records in onshore Renewable Fuels Market since 2017.
Testing has shown some significant data that we are slicing and dicing to better understand these dynamic feedstocks.

## Slide 4: Follow the Feedstock

## Slide 5: Follow the Feedstock
Raw Feed
Need lots of info; dialogue with owners, EPCs, technology providers is key
Clean Feed
Less aggressive cargo if raw feed is cleaned well to maintain purity
Auxiliary
Range of tanks from slop, treatment, chemicals, process water, etc.
Finished Product
Properties similar to crude-based diesel / jet fuels
Storage tanks need to be broken down into categories, with each requiring their own Lining considerations:
Cargo is less aggressive as it moves through the process

## Slide 6: What has changed?
Broad range of feedstocks and products with differing compositions and broad range of storage temperatures (ambient up to 194°F)
Bioethanol
  Impurities
  Water content
Biofuels (+ Feedstock)
  Free Fatty Acid (type and content)
  Water content
More organic material
  Varied composition
  More susceptible to biological attack/decomposition (7-8 times vs. crude)

## Slide 7: Biofuels (+ Feedstock)
Broader range of feedstocks with differing compositions
  Free Fatty Acid (type and content)
      C8 more aggressive than C20
  Water content (%)
  Mineral acid
  Temperature (Loading/Offloading, Storage, Upsets)

## Slide 8: Biofuels (+ Feedstock) Corrosion Risk
Biofuels potentially corrosive to steel
Concerns regarding engineered alloys
MIC reported with Biofuels storage
Water content key to corrosion
Corrosion byproducts could contaminate or consume catalyst in the RDU
Key areas for tank lining discussion:
    Bottom
    Internal Shell
    Underside Roof & Rafters

## Slide 9: Functional Specification
What is to be stored?
  Chemical composition
  Temperature
  Duration
  Purity requirements
  Approvals
What is the substrate and condition?
  Carbon steel – new or pitted
  Stainless steel
  Concrete
What is the lifetime expectancy?
What are the application conditions?
What are the guarantee conditions?

## Slide 10: Generic Specification
Solvent Free Epoxy @ 1 x 20 mils dry film thickness
10% Free Fatty Acid
104°F
2% water

## Slide 11: Free Fatty Acids (FFA)
Solvent Based Epoxy at 140°F
Increasing Free Fatty Acid %
10%
100%
50%

## Slide 12: Free Fatty Acids (FFA)
Solvent Based Epoxy Phenolic with 100% FFA
Increasing Temperature
140°F
176°F
158°F

## Slide 13: Rancidity
Rancidification is the process of complete or incomplete oxidation or hydrolysis of fats and oils when exposed to air, light, or moisture or by bacterial action, resulting in unpleasant taste and odor.
Hydrolytic (with water)
Oxidative (with oxygen)
Oxidative rancidity – oxidation of fatty acid fragments to form aldehydes and ketones
Vegetable oils are mostly Triglycerides . Triglycerides break down increase Fatty Acid content (Water/Temperature/Time)

## Slide 14: Biofuels (+ Feedstock)
Biofuels/FFA and water are not compatible
Over time water layer can accumulate
At higher temperatures can be an issue

## Slide 15: Free Fatty Acids (FFA)
Novolac Vinyl Ester at 178°F
Increasing Free Fatty Acid %
10%
100%
50%

## Slide 16: Technical Specification Summary
Ideal Systems
  Novolac Vinyl Ester systems @ 1 or 2 coats
  Novolac Polycyclamine Cured systems @ 1 coat
  Novolac Epoxy Thin Film systems @ 2 coats
  Vinyl Ester systems @ 1 or 2 coats
Notes: 282HB, 282, 232 405HTR
994, 253
242, 242HB

## Slide 17: Best Practices
Important questions to ask:
  Commodity?
    Chemistry (FFA %, TAN, SDS, Acids, etc.)
    Temperature (Loading/Offloading, Storage, Upsets)
    Heating Elements (Coils or Panels, Location)
    Water Content (%)
    Cargo Purity (Catalyst consumption)
  Tank type?
    Fixed roof, Floating roof, Open top, Metallurgy
  Application equipment?
    Plural component or Single-leg
  Budget?
    Durability, Performance expectations
Keys to success:
  Communication
    Owner
    Technology Provider
    EPC
    Coating/Lining Vendor
    Applicator
  Plan for future feedstock changes
    Dedicated tank
    Mixed tank
    Availability

## Slide 18: Tank Lining Scenarios
Line nothing
  Stainless steel tank, non-corrosive cargo(s), or dedicated cargo(s)
Line bottom and up shell ~ 3 feet
  Carbon steel crude tanks
Line bottom and up shell ~ 3 feet + roof & rafters and down X feet
  No corrosion anticipated in middle and/or floating roof
Line bottom and full shell
  Carbon steel bottoms/shell
  Stainless steel roof & rafters
Line entire tank
  Carbon steel tanks with expected corrosive atmospheres
  Proactive approach to future feedstock needs

## Slide 19: Tank Lining Scenarios
Line nothing
  Stainless steel tank, non-corrosive cargo(s), or dedicated cargo(s)
Line bottom and up shell ~ 3 feet
  Carbon steel crude tanks
Line bottom and up shell ~ 3 feet + roof & rafters and down X feet
  No corrosion anticipated in middle and/or floating roof
Line bottom and full shell
  Carbon steel bottoms + shell
  Stainless steel roof & rafters
Line entire tank
  Carbon steel tanks with expected corrosive atmospheres
  Proactive approach to future feedstock needs

## Slide 20: Tank Lining Scenarios
Line nothing
  Stainless steel tank, non-corrosive cargo(s), or dedicated cargo(s)
Line bottom and up shell ~ 3 feet
  Carbon steel crude tanks
Line bottom and up shell ~ 3 feet + roof & rafters and down X feet
  No corrosion anticipated in middle and/or floating roof
Line bottom and full shell
  Carbon steel bottoms + shell
  Stainless steel roof & rafters
Line entire tank
  Carbon steel tanks with expected corrosive atmospheres
  Proactive approach to future feedstock needs

## Slide 21: Tank Lining Scenarios
Line nothing
  Stainless steel tank, non-corrosive cargo(s), or dedicated cargo(s)
Line bottom and up shell ~ 3 feet
  Carbon steel crude tanks
Line bottom and up shell ~ 3 feet + roof & rafters and down X feet
  No corrosion anticipated in middle and/or floating roof
Line bottom and full shell
  Carbon steel bottoms + shell
  Stainless steel roof & rafters
Line entire tank
  Carbon steel tanks with expected corrosive atmospheres
  Proactive approach to future feedstock needs

## Slide 22: Tank Lining Scenarios
Line nothing
  Stainless steel tank, non-corrosive cargo(s), or dedicated cargo(s)
Line bottom and up shell ~ 3 feet
  Carbon steel crude tanks
Line bottom and up shell ~ 3 feet + roof & rafters and down X feet
  No corrosion anticipated in middle and/or floating roof
Line bottom and full shell
  Carbon steel bottoms + shell
  Stainless steel roof & rafters
Line entire tank
  Carbon steel tanks with expected corrosive atmospheres
  Proactive approach to future feedstock needs

## Slide 23: Lessons Learned
First Renewable Diesel Project (2017)
  Fatty acid (tallow) tank
  Issues were noticed with the tank metallurgy and lining after only 6-months in service
  Lining was applied on floor and up the wall 8 feet
  Suspected challenges with lining installation (and possibly surface preparation), but not confirmed
  Corrosion of shell and vapor phase (mainly) was key reason for tank coming out of service
  New shell courses and entire top of tank replaced
  Entire tank was relined with different lining that was more user-friendly (2-component)
  Opened for inspection in 2021 and looked like day it was re-installed
  Owner currently uses this tried-and-trusted system for all fatty acid (tallow) tanks
Latest Sustainable Aviation Fuel Discussion (June 2022)
  Recent information indicates processing temperatures could be higher to reduce usage of costly catalyst
  Likely will impact the current metallurgy and/or linings used in the industry
Notes: Surface prep and application issues

## Slide 24: Lessons Learned 2017
Notes: Surface prep and application issues

## Slide 25: Lessons Learned 2018
Notes: Surface prep and application issues

## Slide 26: Key Takeaways
Raw Feed
Potentially very aggressive cargo, combined with elevated temperatures
Clean Feed
Less aggressive cargo, if raw feed is cleaned well to maintain purity
Auxiliary
Slops, treatment, chemicals, process water, etc.
Finished Product
Properties similar to crude-based diesel / jet fuels
Infrastructure needs to be broken down into categories, with each requiring their own Lining considerations:
Raw Feed
Clean Feed
Auxiliary
Finished Product

## Slide 27: Industry Quotes…
“Feedstocks are dynamic, even in storage”
“Gremlins exist in these feedstocks”
“Heat, water, and oxygen will drive rancidity”
“Significant corrosion exists in the vapor phase”
“Material selection is critical due to high corrosion mechanisms”

## Slide 28: Thank You!
The use of polymeric coatings in storage and handling (before processing) as well as pretreatment:
Problematic areas where non-metallics may be a solution
Current coatings used in biofuels Railcars, Storage tanks and Process vessels